Specifications of CFO-xx-OM2-xxM Multimode 50/125um optical fibre cables

| Characteristics | Conditions | Value [units] |
| --- | --- | --- |
| Optical characteristics |  |  |
| Attenuation | 850nm | ≤3.0 [dB/km] |
|  | 1300nm | ≤1.0 [dB/km] |
| Overfilled Modal Bandwidth | 850nm | ≥200 [MHz x km] |
|  | 1300nm | ≥500 [MHz x km] |
| Numerical Aperture (NA) |  | 0.200±0.015 |
| Group index of refraction (Typical) | 850nm | 1.482 |
|  | 1300nm | 1.477 |
| Geometrical characteristics |  |  |
| Core diameter |  | 50±2.5 [um] |
| Cladding diameter |  | 125.0±1.0 [um] |
| Cladding non-circularity |  | ≤1.0 % |
| Coating diameter |  | 242±7 [um] |
| Coating/ cladding concentricity error |  | ≤12.0 [um] |
| Coating non-circularity |  | ≤6.0 % |
| Core/ cladding concentricity error |  | ≤1.5 [um] |
| Environmental characteristics at 850nm, 1300nm |  |  |
| Temperature dependence induced attenuation | -60℃ to +85 ℃ | ≤0.10 [dB/km] |
| Temperature humidity cycling induced attenuation | -10℃ to +85℃, 90% R.H | ≤0.20 [dB/km] |
| Damp heat dependence induced attenuation | 85℃, 85% R.H., 30 days | ≤0.20 [dB/km] |
| Watersoak dependence induced attenuation | 20℃ for 30 days | ≤0.20 [dB/km] |